Mapping Report

Condition

| Acquire Date | 6/18/2018 9:36:49 AM | Voltage | 50 kV |
| --- | --- | --- | --- |
| Scan Size | 8.640, 12.810 mm | Current | 1000 uA |
| Image size | 288 x 427 pixel | Filter | OFF |
| Pixel size | 30 um/pixel | Collimator | 0.2x0.2mm |
| Time per pixel | 50.00 ms |  |  |
| Frame Accmu. counts | 1 |  |  |
| Mapping Total Time | 104.7 min |  |  |

Sample image

Ca-Ka

P-Ka

Fe-Ka

Mn-Ka

Sr-Ka

K-Ka

Zn-Ka